| PHYSICAL SPECIFICATION |
| --- |
| Nominal Voltage Nominal Capacity (20HR) | 6V 1Ah |  |
| Dimension | Length Width Container Height Total Height | 51±1mm （2.01 inches） 42±1mm (1.65 inches) 51±1mm (2.01 inches) 56±1mm (2.20 inches) |  |
| Weight | Approx. 0.25 Kg ( 0.55lbs) |  |
| Standard Terminal | Fasten Tab No.187E |  |
| ELECTRICAL SPECIFICATION |
| Characteristics | Discharge curves @ 25℃ (77 °F) |
| Capacity | 20 hour rate (0.05A) 10 hour rate (0.09A) 5 hour rate (0.17A) 3 hour rate (0.25A) 1hour rate (0.6A) | 1Ah 0.95Ah 0.85Ah 0.75Ah 0.6Ah |  |
| Capacity affected by temperature | 40℃ （104 0F） 25℃ （77 0F） 0℃ （32 0F） | 102% 100% 85% |  |
| Internal Resistance | Full charged battery (25℃,77 0F) 35mΩ |  |
| Constant Voltage Charge | Cycle | Initial Charging Current less than 0.3A Voltage 7.20~7.50V at 25℃ (77 0F ) Temperature Coefficient –15mV/℃ |  |
|  | Standby | No limit on Initial Charging Current Voltage 6.75~6.90V at 25℃ (77 0F ) Temperature Coefficient –10mV/℃ |  |