| PHYSICAL SPECIFICATION |
| --- |
| Nominal Voltage Nominal Capacity (20HR) | 6V 16Ah |  |
| Dimension | Length Width Container Height Total Height | 108±1mm （4.25 inches） 71±1mm (2.80 inches) 139±1mm (5.47 inches) 139±1mm (5.47 inches) |  |
| Weight | Approx. 2.54Kg ( 5.60lbs) |  |
| Standard Terminal | Connector |  |
| ELECTRICAL SPECIFICATION |
| Characteristics | Discharge curves @ 25℃ (77 °F) |
| Capacity | 20 hour rate (0.8A) 10 hour rate (1.44A) 5 hour rate (2.72A) 3 hour rate (4A) 1hour rate (9.6A) | 16Ah 15.2Ah 13.6Ah 12Ah 9.6Ah |  |
| Capacity affected by temperature | 40℃ （104 0F） 25℃ （77 0F） 0℃ （32 0F） | 102% 100% 85% |  |
| Internal Resistance | Full charged battery (25℃,77 0F) 10mΩ |  |
| Constant Voltage Charge | Cycle | Initial Charging Current less than 4.8A Voltage 7.20~7.50V at 25℃ (77 0F ) Temperature Coefficient –15mV/℃ |  |
|  | Standby | No limit on Initial Charging Current Voltage 6.75~6.90V at 25℃ (77 0F ) Temperature Coefficient –10mV/℃ |  |