| PHYSICAL SPECIFICATION |
| --- |
| Nominal Voltage Nominal Capacity (20HR) | 8V 3Ah |  |
| Dimension | Length Width Container Height Total Height | 134±1mm (5.28 inches) 36±1mm (1.42 inches) 64±1mm (2.52 inches) 69±1mm (2.72 inches) |  |
| Weight | Approx. 0.84 Kg ( 1.85lbs) |  |
| Standard Terminal | Fasten Tab No.187E |  |
| ELECTRICAL SPECIFICATION |
| Characteristics | Discharge curves @ 25℃ (77 °F) |
| Capacity | 20 hour rate (0.15A) 10 hour rate (0.27A) 5 hour rate (0.51A) 3 hour rate (0.75A) 1hour rate (1.8A) | 3Ah 2.85Ah 2.55Ah 2.25Ah 1.8Ah |  |
| Capacity affected by temperature | 40℃ （104 0F） 25℃ （77 0F） 0℃ （32 0F） | 102% 100% 85% |  |
| Internal Resistance | Full charged battery (25℃,77 0F) 25mΩ |  |
| Constant Voltage Charge | Cycle | Initial Charging Current less than 0.9A Voltage 9.6~10V at 25℃ (77 0F ) Temperature Coefficient –18mV/℃ |  |
|  | Standby | No limit on Initial Charging Current Voltage 9~9.2V at 25℃ (77 0F ) Temperature Coefficient –18mV/℃ |  |