| PHYSICAL SPECIFICATION |
| --- |
| Nominal Voltage Nominal Capacity (20HR) | 6V 5Ah |  |
| Dimension | Length Width Container Height Total Height | 70±1mm （2.76 inches) 47±1mm (1.85 inches) 100±1mm (3.94 inches) 106±1mm (4.17 inches) |  |
| Weight | Approx. 0.79Kg ( 1.74lbs) |  |
| Standard Terminal | F1-Fasten Tab No.187E |  |
| ELECTRICAL SPECIFICATION |
| Characteristics | Discharge curves @ 25℃ (77 °F) |
| Capacity | 20 hour rate (0.25A) 10 hour rate (0.45A) 5 hour rate (0.85A) 3 hour rate (1.25A) 1hour rate (3A) | 5Ah 4.7Ah 4.3Ah 3.8Ah 3Ah |  |
| Capacity affected by temperature | 40℃ （104 0F） 25℃ （77 0F） 0℃ （32 0F） | 102% 100% 85% |  |
| Internal Resistance | Full charged battery (25℃,77 0F) 25mΩ |  |
| Constant Voltage Charge | Cycle | Initial Charging Current less than 1.5A Voltage 7.20~7.50V at 25℃ (77 0F ) Temperature Coefficient –15mV/℃ |  |
|  | Standby | No limit on Initial Charging Current Voltage 6.75~6.90V at 25℃ (77 0F ) Temperature Coefficient –10mV/℃ |  |