| PHYSICAL SPECIFICATION |
| --- |
| Nominal Voltage Nominal Capacity (10HR) | 2V 150Ah |  |
| Dimension | Length Width Container Height Total Height | 171±2mm （6.73 inches） 102±2mm (4.02 inches) 205±2mm (8.07 inches) 227±2mm (6.94 inches) |  |
| Weight | Approx. 9.5 Kg ( 20.9lbs) |  |
| Standard Terminal | Bolt-and-nuts terminal Bolt Type: M8 |  |
| ELECTRICAL SPECIFICATION |
| Characteristics | Discharge curves @ 25℃ (77 °F) |
| Capacity | 100 hour rate (1.5A) 50 hour rate (3A) 10 hour rate (15A) 1hour rate (97.5A) | 165Ah 157Ah 150Ah 98Ah |  |
| Capacity affected by temperature | 40℃ （104 0F） 25℃ （77 0F） 0℃ （32 0F） | 102% 100% 85% |  |
| Designed life | ≥4000Cycles @ 20% DOD(25℃) |  |
| Internal Resistance | Full charged battery (25℃,77 0F) 0.9mΩ |  |
| Constant Voltage Charge | Cycle | Initial Charging Current less than 37.5A Voltage 2.35~2.40V at 25℃ (77 0F ) Temperature Coefficient –5mV/℃ |  |
|  | Standby | No limit on Initial Charging Current Voltage 2.25~2.30V at 25℃ (77 0F ) Temperature Coefficient –3.3mV/℃ |  |